| IMIVBR20 Carry out motor vehicle body resistance spot welding operations |  |
| --- | --- |

Overview

This standard is about joining materials correctly and effectively using resistance spot welding techniques.

Performance criteria

You must be able to:

P1

‍

use the appropriate

personal protective equipment (PPE)

and check it is fit for purpose before carrying out resistance spot welding operations

P2

‍

protect the vehicle, its systems and its contents effectively when carrying out resistance spot welding operations

P3

‍

prepare material and align to enable suitable join to be achieved, ensuring mating flanges are treated following manufacturers’ procedures before joining

P4

‍

select, set up and use the correct

tools

and equipment

in order to correctly carry out resistance spot welding operations

P5

‍

ensure that the

tools

,

equipment

and

PPE

you require are in a safe working condition and are correct for the joining operation that you are to be completing

P6

‍

set up your

equipment

to carry out spot welding operations checking:

P6.1

‍

suitability of the air supply and pressure

P6.2

‍

the current supply

P6.3

‍

the consumables are correct

P6.4

‍

the suitability/serviceability of electrodes and tips

P7

‍

carry out spot welding operations following:

P7.1

‍

recognised researched repair methods

P7.2

‍

test procedures in accordance with British Standards (peel/sheer/nugget size)

P7.3

‍

manufacturer's processes, methods and procedures

P7.4

‍

your workplace processes, methods and procedures

P7.5

‍

health, safety and legal requirements

P8

‍

avoid damaging other components, standards, panels and surfaces on the vehicle and the surrounding work area

P9

‍

recognise when your weld is not forming correctly and what action needs to be taken

P10

‍

inspect and assess resistance spot weld quality in accordance to British Standards, including weld pitch, indention/weld profile, heat zone, nugget size and peel and shear test

P11

‍

check integrity of weld and record the type of weld achieved on the appropriate paper work. Test pieces must be recorded and stored

P12

‍

dress and protect the repaired area to inhibit corrosion where applicable

P13

‍

clean and store

PPE

and

equipment

in appropriate manner

P14

‍

promptly report any additional faults you notice during the course of your work to the relevant person(s)

P15

‍

promptly report any delays in completing your work to the relevant person(s)

P16

‍

carry out resistance spot welding operations within the agreed timescale

P17

‍

complete work records accurately, in the format required and promptly pass them to the relevant person(s)

Knowledge and understanding

You need to know and understand:

K1

‍

the health, safety and legal requirements relating to the joining of materials using resistance spot welding techniques

K2

‍

your workplace procedures for carrying out appropriate risk assessment(s), the referral of problems, reporting of delays to the completion of work and completion of work records

K3

‍

the constraints of the type of materials used in vehicle construction places on the choice of repair

equipment

*

K4

‍

how to prepare, test and adjust all *

equipment

required for resistance spot welding techniques

K5

‍

the work that needs to be done and the standard required

K6

‍

the requirements for protecting the vehicle and contents from damage before, during and after the joining of materials using resistance spot welding techniques

K7

‍

the importance of selecting, using, maintaining and storing the appropriate

PPE

when the joining of materials using resistance spot welding techniques

K8

‍

how to find, interpret and use sources of information (including repair methods) applicable to the joining of materials using resistance spot welding techniques  and the implications of not fully understanding the repair methods presented

K9

‍

how to select, check, maintain, set up and store all of the

tools

and equipment

required to correctly join materials using resistance spot welding techniques

K10

‍

the different types of welding processes, techniques and joints used for the joining of materials when using resistance spot welding techniques

K11

‍

the correct surface preparation methods to ensure the correct resistance spot weld is achieved and the reasons why surface preparation is important

K12

‍

the faults and defects that can occur when carrying out resistance spot welding and the common causes of these faults

K13

‍

the need for correct alignment of materials and the methods used to achieve this

K14

‍

the types of quality control checks that can be used to ensure correct joining of materials e.g. test coupons

K15

‍

how to inspect and assess resistance weld quality in accordance to British Standards including weld pitch, indention/weld profile, heat zone, nugget size, peel and shear test

K16

‍

the correct use of adhesives with resistance spot welding techniques

K17

‍

the implications of electro-magnetic fields and the effects on medical devices

Scope/range

All of the items listed below form part of this National Occupational Standard.

1.

‍

**Personal protective equipment (PPE)** for resistance spot welding operations includes: